No. 2178-83 CycLoops( Twist( Bicycle Rack

Bicycle Rack shall be CycLoops Twist in the material, color finish and mounting style selected by the owner's representative and in the quantity shown on the bill of materials or the project drawings.  Manufacturer, Columbia Cascade Company, 1300 SW Sixth Avenue, Suite 310, Portland OR 97201-3464 U.S.A.

1.  Materials

Bicycle Rack shall be one-piece 1-1/2-inch i.d. schedule 40 mild steel or stainless steel seamless pipe with a minimum wall thickness of .145 inch.  Easily vandalized thin wall tubing is not allowed.  Embedment (-E) mount (permanent) legs shall extend ten inches below finished grade and be drilled prior to application of finish to accept No. 4 re-bar furnished by installing contractor.  Surface mount 

(-SM) shall include holes in each base to accept anchoring devices furnished by installing contractor.

2.  Construction

Bicycle Rack shall have a twisted shape derived from smooth 1’-5/16” radius mandrel bends. Bending that distorts the pipe is not allowed.  Bicycle Rack shall be deburred and ground smooth after fabrication.  

3.  Finish

Rack shall be coated with CASPAX-7(, a tough, opaque, UV resistant exterior grade polyester powder coating applied to a minimum thickness of 6 mils.  Liquid, epoxy or lead-containing powder coatings are not acceptable.   

Preparation of the mild steel substrate shall incorporate the phosphate system.  Substrate preparation shall consist first of mechanical cleaning to remove heavy mill scale, rust, varnish, grease, etc., with surfaces uniformly abraded to promote quality of finish coating.  Chemical cleaning in accordance with TT-C-490C, Methods I and III shall remove impurities from the surfaces.  

After the two-step cleaning process, the metal substrate shall receive a corrosion-inhibiting iron phosphate pre-coating in accordance with TT-C-490C, Type II, prior to the application of the powder color coat.  The color coating shall be applied by the electrostatic method and then oven-cured at 400 degrees Fahrenheit to chemically bond the coating to the substrate and to render the coated metal resistant to abrasion, impact, chipping, weathering, and rusting.


-or-

Stainless steel pipe shall have No. 4 polish finish.

© 2011 Columbia Cascade Company.  No portion of this publication may be reproduced without prior authorization.  Authorization is hereby granted for photocopies to be made and              distributed to those involved in the specification of TimberForm products.


